## Slide 1
CORMAC TOHER
COREY OSES
DAVID HICKS
E. Gossett,
F. Rose,
S. Curtarolo
Materials Science
Duke University
AFLOW: Integrated infrastructure for computational materials discovery
E

## Slide 2
Outline
Getting started with AFLOW:
  Decorating crystal prototypes to set up new calculations
  Symmetry analysis
Thermodynamic and thermo-mechanical
  Convex hull phase diagrams
  AEL/AGL/APL: Elastic constants and thermal properties
AFLOW online data repositories
  AFLOW.org online web interface
  AFLOW REST-API
  AFLUX Search-API
AFLOW-ML + API
AFLOW code:
  Installing AFLOW
  Data analysis with AFLOW
  Running AFLOW calculations

## Slide 3
Outline
Getting started with AFLOW:
  Decorating crystal prototypes to set up new calculations
  Symmetry analysis
Thermodynamic and thermo-mechanical
  Convex hull phase diagrams
  AEL/AGL/APL: Elastic constants and thermal properties
AFLOW online data repositories
  AFLOW.org online web interface
  AFLOW REST-API
  AFLUX Search-API
AFLOW-ML + API
AFLOW code:
  Installing AFLOW
  Data analysis with AFLOW
  Running AFLOW calculations

## Slide 4
Automated Materials Discovery
Automated computational materials discovery:
Experimental structures
Automated QM calculations
Searchable/sortable database
Candidate materials
Structural prototypes
ML models
Density functional theory

## Slide 5
AFLOW: Automatic FLOW
AFLOW
DFT-code
aflow.in
Elastic
Electronic
Thermal
Storage
Property calculation
Database storage
Calculation management
Input file generation
DFT-code
DFT-code
DFT-code
ERROR?
Curtarolo et al., Comput. Mater. Sci. 58, 218 (2012); Calderon et al., Comp. Mat. Sci. 108A, 233 (2015)
AFLOW source code now available under GPL 3
materials.duke.edu/AFLOW/

## Slide 6
AFLOW.org: web portal
http://aflow.org
Machine-learning model
Convex hull
AFLOW-online
(AFLOW-SYM)
Crystal Prototypes
Curtarolo et al., Comput. Mater. Sci. 58, 218 (2012); Curtarolo et al., Comput. Mater. Sci. 58, 227 (2012)
> 1.8 million entries
Advanced Search

## Slide 7
AFLOW: Crystallographic Prototypes
G (p, T; V) = E + pV
AFLOW contains built-in structural prototypes:
Decorating prototypes with different elements allows for automated creation of new hypothetical materials
~600 prototypes available at aflow.org/CrystalDatabase
Prototype T0001: Heusler structure
Prototype T0002:
Anti-Heusler structure
Prototype T0003:
Half-Heusler structure
M. J. Mehl et al., Comput. Mater. Sci. 136, S1-S828 (2017); D. Hicks et al., submitted (2018)

## Slide 8
AFLOW: Crystallographic Prototypes
http://aflow.org
Crystal Prototypes
M. J. Mehl et al., Comput. Mater. Sci. 136, S1-S828 (2017); D. Hicks et al., submitted (2018)

## Slide 9
AFLOW: Crystallographic Prototypes
M. J. Mehl et al., Comput. Mater. Sci. 136, S1-S828 (2017); D. Hicks et al., submitted (2018)

## Slide 10
AFLOW: Crystallographic Prototypes
G (p, T; V) = E + pV
M. J. Mehl et al., Comput. Mater. Sci. 136, S1-S828 (2017); D. Hicks et al., submitted (2018)
Jmol interface
Prototype information

## Slide 11
AFLOW: Crystallographic Prototypes
G (p, T; V) = E + pV
M. J. Mehl et al., Comput. Mater. Sci. 136, S1-S828 (2017); D. Hicks et al., submitted (2018)
Atomic basis vectors
Primitive lattice vectors
References
Geometry files

## Slide 12
AFLOW: Crystallographic Prototypes
G (p, T; V) = E + pV
M. J. Mehl et al., Comput. Mater. Sci. 136, S1-S828 (2017); D. Hicks et al., submitted (2018)
Format options
Prototype generator
Structure output
AFLOW command

## Slide 13
AFLOW: Crystallographic Prototypes
G (p, T; V) = E + pV
Exercises:
Select a prototype from the Library of Crystallographic Prototypes at aflow.org/ CrystalDatabase/. Use the online tool to create a POSCAR for that structure, decorated with elements of your choice.
Generate structures for the prototype A_hR1_166_a using an element and value of a of your choice, with c/a values of 0.5, 0.612, 1.0, 1.225, 1.5, 2.45, and 3.0. Save these structures with appropriate names, as they will be used as part of a later exercise.
M. J. Mehl et al., Comput. Mater. Sci. 136, S1-S828 (2017); D. Hicks et al., submitted (2018)

## Slide 14
AFLOW-SYM
G (p, T; V) = E + pV
D. Hicks et al., Acta Cryst. A74, 184-203 (2018)
AFLOW-SYM tests invariance of crystal under transformations
Provides information on space group, Pearson symbol, Bravais lattice, primitive and conventional cell, etc.
API keywords: spacegroup_relax, Pearson_symbol_relax, Bravais_lattice_orig, …

## Slide 15
AFLOW-SYM
G (p, T; V) = E + pV
D. Hicks et al., Acta Cryst. A74, 184-203 (2018)
Mismatch with respect to space group listed in description of experimental structure in ICSD

## Slide 16
AFLOW-SYM
G (p, T; V) = E + pV
D. Hicks et al., Acta Cryst. A74, 184-203 (2018)
AFLOW-SYM performs self-consistent tolerance scan when transformations are inconsistent with ITC space groups, or when inconsistencies exist between different representations.

## Slide 17
AFLOW-SYM
D. Hicks et al., Acta Cryst. A74, 184-203 (2018)
AFLOW-SYM consists of robust mapping procedure; takes lattice skewness into account
minimum in fractional ≠ minimum in Cartesian
Cartesian
fractional
cubic
orthorhombic
triclinic
Cartesian
fractional

## Slide 18
AFLOW-SYM: AFLOW-Online
http://aflow.org
AFLOW-online
(AFLOW-SYM)
D. Hicks et al., Acta Cryst. A74, 184-203 (2018)

## Slide 19
AFLOW-SYM: AFLOW-Online
D. Hicks et al., Acta Cryst. A74, 184-203 (2018)
Enter POSCAR here
Select AFLOW-SYM here
Submit here when ready

## Slide 20
AFLOW-SYM
G (p, T; V) = E + pV
Exercises:
Use AFLOW-SYM to determine the symmetry properties of the structure that you generated using prototype you selected from the Library of Crystallographic Prototypes at aflow.org/CrystalDatabase/. What are the space group number and Pearson symbol for this material?
Use AFLOW-SYM to determine the symmetry properties of the structures that you generated for the prototype A_hR1_166_a. How do the choice of parameters affect the symmetry of the structure?
D. Hicks et al., Acta Cryst. A74, 184-203 (2018)

## Slide 21
Outline
Getting started with AFLOW:
  Decorating crystal prototypes to set up new calculations
  Symmetry analysis
Thermodynamic and thermo-mechanical
  Convex hull phase diagrams
  AEL/AGL/APL: Elastic constants and thermal properties
AFLOW online data repositories
  AFLOW.org online web interface
  AFLOW REST-API
  AFLUX Search-API
AFLOW-ML + API
AFLOW code:
  Installing AFLOW
  Data analysis with AFLOW
  Running AFLOW calculations

## Slide 22
AFLOW-CHULL: Convex Hull Phase Diagram
G (p, T; V) = E + pV
Convex hull phase diagram: formation enthalpy vs. concentration
\Delta H (A_{N_{\mathrm A}} B_{N_{\mathrm B}}) = H (A_{N_{\mathrm A}} B_{N_{\mathrm B}}) - (N_{\mathrm A}H(A) + N_{\mathrm B} H(B))
\Delta H (A_{x_{\mathrm A}} B_{x_{\mathrm B}}) = H (A_{x_{\mathrm A}} B_{x_{\mathrm B}}) - (x_{\mathrm A}H(A) + x_{\mathrm B} H(B))
API keywords: enthalpy_formation_atom, energy_cell, …
C. Oses et al., submitted arXiv:1806.06901 (2018)

## Slide 23
AFLOW-CHULL: Convex Hull Phase Diagram
Ternary convex hull phase diagrams:
Interactive online application: aflow.org/aflow-chull
C. Oses et al., submitted arXiv:1806.06901 (2018)

## Slide 24
AFLOW-CHULL: Data curation
C. Oses et al., submitted arXiv:1806.06901 (2018)
outlier detection and removal
Te3Zr1_ICSD_42076
Te3Zr1_ICSD_653211
Te3Zr1_ICSD_653232
Te3Zr1_ICSD_51004
Te3Zr1_ICSD_71033
Te3Zr1_ICSD_86763
Te3Zr1_ICSD_86764
structure match

## Slide 25
AFLOW-CHULL: Thermodynamic analyses
C. Oses et al., submitted arXiv:1806.06901 (2018)
decomposition reaction
stability criterion
\mathrm{Pd}_{2}\mathrm{Pt}_{3} \to 1.5 ~ \mathrm{PdPt} + 0.5 ~ \mathrm{PdPt}_{3}
\Delta H_{\mathrm{f}} = 3~\mathrm{meV/atom}
\delta_{\mathrm{sc}}=6~\mathrm{meV/atom}

## Slide 26
AFLOW-CHULL: Convex Hull Phase Diagram
G (p, T; V) = E + pV
aflow --chull --alloy=AgAuCd
C. Oses et al., submitted arXiv:1806.06901 (2018)
Go to aflow.org/aflow-chull and type/select AgAuCd

## Slide 27
AFLOW-CHULL: Convex Hull Phase Diagram
G (p, T; V) = E + pV
Click “Download PDF”
aflow --chull --alloy=AgAuCd
C. Oses et al., submitted arXiv:1806.06901 (2018)

## Slide 28
AFLOW-CHULL: Convex Hull Phase Diagram
G (p, T; V) = E + pV
aflow --chull --alloy=AgAuCd
C. Oses et al., submitted arXiv:1806.06901 (2018)
Click “Highlight Hull Points” and click on one

## Slide 29
AFLOW-CHULL: Convex Hull Phase Diagram
G (p, T; V) = E + pV
aflow --chull --alloy=AgAuCd
C. Oses et al., submitted arXiv:1806.06901 (2018)
Click “Highlight Hull Points” and click on one

## Slide 30
AFLOW-CHULL: Convex Hull Phase Diagram
G (p, T; V) = E + pV
Exercises:
What is the distance of Al17Co12 from the hull?
What is the stability criterion of Te2Zr?
What is the energy of the CuZr hull at x = 0.5?
What is the most stable structure on the MnPdPt hull?
C. Oses et al., submitted arXiv:1806.06901 (2018)

## Slide 31
Apply set of independent normal and shear strains
Normal strain
Shear strain
Use strain-stress data to calculate elastic properties:
  6x6 elastic tensors
  Bulk and shear modulus
  Poisson ratio
  Combine with AGL (Debye model) to get more accurate Debye temperature and thermal conductivity
AEL: Elastic constants
C. Toher et al., Phys. Rev. Mater. 1, 015401 (2017)

## Slide 32
…, , , ,…
Different volume cells
E(V) data from DFT
(VASP, QE, etc.)
Fit with polynomial or eqn of state: bulk modulus, B(V)
AGL: Debye-Grüneisen model
C. Toher et al., Phys. Rev. B 90, 174107 (2014); M. A. Blanco et al., Comp. Phys. Commun. 158, 57 (2004)
B_S (V) &\approx V \left( \frac{\partial^2 E(V)}{\partial V^2} \right)
Debye temperature: θD(V)
Grüneisen parameter: γ
Lattice thermal conductivity, κL
Heat capacity: CV

## Slide 33
Thermal Conductivity (300K)
AGL+AEL: Results
Debye temperature
Correlation with experimental results is ~0.9
Using AEL Poisson ratio improves correlation by ~5%
AGL method suited for rapid screening of thermal properties
C. Toher et al., Phys. Rev. B 90, 174107 (2014); C. Toher et al., Phys. Rev. Mater. 1, 015401 (2017)

## Slide 34
APL: Phonon calculations
Perturb atom, obtain change in force on others
\Phi_{ij}^{\alpha \beta } &= \frac{\partial^2V}{\partial r_{i}^{\alpha} \partial r_{j}^{\beta} }
\Phi_{ijk}^{\alpha \beta \gamma} &= \frac{\partial^3V}{\partial r_{i}^{\alpha} \partial r_{j}^{\beta} \partial r_{k}^{\gamma}}
AFLOW Phonon Library
Interatomic force constants
Phonon dispersion
D_{ij}^{\alpha \beta }(\mathbf{q}) = \sum_l \frac{\Phi(i,j)_{\alpha \beta}}{\sqrt{M(i)M(j)}}\exp\left[-i\mathbf{q} \cdot \left(\mathbf{R}_{l}-\mathbf{R}_{0}\right)\right]
\omega_{\lambda}, e_{\lambda}
Curtarolo et al., Comput. Mater. Sci. 58, 218 (2012); Curtarolo et al., Comput. Mater. Sci. 58, 227 (2012)

## Slide 35
AEL-AGL combined workflow has been run for > 5000 materials
Data is accessible online at aflow.org, via AFLOW REST-API and AFLUX search-API
Elastic property keywords: ael_bulk_modulus_vrh, ael_shear_modulus_vrh, ael_poisson_ratio, …
Thermal properties keywords: agl_debye, agl_gruneisen, agl_heat_capacity_Cv_300K, agl_thermal_conductivity_300K, agl_thermal_expansion_300K, …
AFLOW.org: Thermo-mechanical properties
C. Toher et al., Phys. Rev. Mater. 1, 015401 (2017)

## Slide 36
Outline
Getting started with AFLOW:
  Decorating crystal prototypes to set up new calculations
  Symmetry analysis
Thermodynamic and thermo-mechanical
  Convex hull phase diagrams
  AEL/AGL/APL: Elastic constants and thermal properties
AFLOW online data repositories
  AFLOW.org online web interface
  AFLOW REST-API
  AFLUX Search-API
AFLOW-ML + API
AFLOW code:
  Installing AFLOW
  Data analysis with AFLOW
  Running AFLOW calculations

## Slide 37
AFLOW.org: web portal
http://aflow.org
Machine-learning model
Convex hull
AFLOW-online
(AFLOW-SYM)
Crystal Prototypes
Curtarolo et al., Comput. Mater. Sci. 58, 218 (2012); Curtarolo et al., Comput. Mater. Sci. 58, 227 (2012)
> 1.8 million entries
Advanced Search

## Slide 38
AFLOW.org: search page
http://aflow.org/advanced.php
Element selection
Property Filters
Number of species
Element group selection
R. H. Taylor et al., Comput. Mater. Sci. 93, 178-192 (2014)

## Slide 39
AFLOW.org: search page
http://aflow.org/advanced.php
Number of species=2
Added filter for Egap: electronic band bap
Selected Elements
R. H. Taylor et al., Comput. Mater. Sci. 93, 178-192 (2014)
Check box to restrict search results to specific value range

## Slide 40
AFLOW.org: search page
G (p, T; V) = E + pV
Exercises:
Use the advanced search functionality to find the band gap for SiC in the zincblende structure (space group number 216).
Use the advanced search functionality to find the bulk moduli for materials containing Ti in the AFLOW database. How many results are returned?
Use the “Restrict Value” button to limit the search to only entries for which the bulk modulus has already been calculated for materials containing Ti. Open the entry page of the material with the highest bulk modulus. What is the lattice type and space group of this material? Is it a metal or an insulator?
R. H. Taylor et al., Comput. Mater. Sci. 93, 178-192 (2014)

## Slide 41
AFLOW.org: database organization
R. H. Taylor et al., Comput. Mater. Sci. 93, 178-192 (2014)

## Slide 42
AFLOW: REST-API
R. H. Taylor et al., Comput. Mater. Sci. 93, 178-192 (2014)

## Slide 43
AFLOW.org: web portal
Full list of API keywords is available in the online REST-API documentation wiki:
R. H. Taylor et al., Comput. Mater. Sci. 93, 178-192 (2014)
Keywords lists

## Slide 44
AFLOW: REST-API
R. H. Taylor et al., Comput. Mater. Sci. 93, 178-192 (2014)
The AFLOW REST-API AFLOW URL (AURL) has the form:
<server>:AFLOWDATA/<project>/<set>/<entry>/?<keyword>
For example, the AURL for the formation enthalpy per atom of the ternary Heusler structure T0001.A2BC with composition Cu2TiZn is:
aflowlib.duke.edu:AFLOWDATA/LIB3_RAW/Cu_pvTi_svZn/T0001.A2BC/?enthalpy_formation_atom
Server
Entry
Project Layer
Set Layer
Keyword
The URL for the formation enthalpy per atom of the ternary Heusler structure T0001.A2BC with composition Cu2TiZn is:
aflowlib.duke.edu/AFLOWDATA/LIB3_RAW/Cu_pvTi_svZn/T0001.A2BC/?enthalpy_formation_atom
The full list of entries in the set Cu-Ti-Zn can be retrieved using:
aflowlib.duke.edu/AFLOWDATA/LIB3_RAW/Cu_pvTi_svZn/?aflowlib_entries

## Slide 45
AFLOW: REST-API
R. H. Taylor et al., Comput. Mater. Sci. 93, 178-192 (2014)
Example python script to access API & download space groups (see AFLOW_REST_API_example.py):
#!/usr/bin/env python
import json, sys, os
from urllib import urlopen
SERVER="http://aflowlib.duke.edu/AFLOWDATA"
PROJECT="/LIB3_RAW"
SET="/Cu_pvTi_svZn"
ENTRIES="/?aflowlib_entries"
response=urlopen( SERVER+PROJECT+SET+ENTRIES ).read()
response=response.rstrip()
entry_list=response.split(",")
print(entry_list)
for i in xrange(len(entry_list)):
entry=str(entry_list[i])
URLentry_sg=SERVER+PROJECT+SET+"/"+entry+"/?spacegroup_relax"
print(URLentry_sg)
response=urlopen( URLentry_sg ).read()
print(response)
Project: Ternary alloys
Set: CuTiZn alloy system
Keyword: List of entries in this alloy system
Download list of entries with urlopen
Loop through list of entries
Download space group for each entry

## Slide 46
AFLOW: REST-API
G (p, T; V) = E + pV
Exercises:
Use the AFLOW REST-API to download the formation enthalpies for all of the entries in the ternary alloy system AlNiTi (AlNi_pvTi_sv).
Use the AFLOW REST-API to download the full list of binary alloy systems that are available in the LIB2 project. How many alloys systems are available for download?
Use the AFLOW REST-API to download the stoichiometries and space groups for all of the entries in an alloy system of your choice. How many entries are present in this system?
R. H. Taylor et al., Comput. Mater. Sci. 93, 178-192 (2014)

## Slide 47
Aim: Programatically expose the same functionality as our web search interface at http://aflow.org/advanced.php
AFLUX: AFLOW Search-API
Logical operator | LUX syntax
<block> | “(” and “)”
<AND> | “,”
<OR> | “:”
<NOT> | “!”
<loose> | “*”
<string> | “’”
<mute> | “$”
F. Rose et al., Comput. Mater. Sci. 137, 362 (2017).

## Slide 48
AFLUX: AFLOW Search-API
AFLUX enables search functionality through query part of URI
Supports use of several logical operators
Operator scope can be inter-property and/or intra-property
Logical operator | AFLUX syntax | Operator scope
<block> | “(” and “)” | Intra- and inter-property
<AND> | “,” | Intra- and inter-property
<OR> | “:” | Intra- and inter-property
<NOT> | “!” | Intra-property
<loose> | “*” | Intra-property
<string> | “’” | Inter-property
<mute> | “$” | Intra-property
F. Rose et al., Comput. Mater. Sci. 137, 362 (2017).

## Slide 49
AFLUX: AFLOW Search-API
http://aflowlib.duke.edu/search/API/?<matchbook>,<directives>
Search API Server
Query
F. Rose et al., Comput. Mater. Sci. 137, 362 (2017).
Matchbook:
  Materials keywords with arguments
  Example: <server>/?species((Na:K),Cl),nspecies(2),Egap(1*,*5),energy_cell
  Keyword list available from schema directive: <server>/?schema
Directives:
  Formatting instructions with arguments
  “format” takes arguments “json” and “html”
  “catalog” takes arguments “icsd”, “lib1”, “lib2”, ...
  “paging” controls number of entries and page displayed, sorted in ascending order of first materials keyword – order can be reversed by using a negative page number in the argument

## Slide 50
AFLUX: AFLOW Search-API
Example python script to access AFLUX search-API (see AFLUX_example.py):
#!/usr/bin/env python
import json, sys, os
from urllib import urlopen
SERVER="http://aflowlib.duke.edu"
API="/search/API/?"
MATCHBOOK="species((Na:K),Cl),nspecies(2),Egap(2*,*5),energy_cell"
DIRECTIVES="$paging(0)"
SUMMONS=MATCHBOOK+","+DIRECTIVES
response=json.loads(urlopen(SERVER+API+SUMMONS).read().decode("utf-8"))
for datum in response:
bandgap=[float(x) for x in datum['Egap'].split(",")]
energycell=[float(x) for x in datum['energy_cell'].split(",")]
print ("{}, {}, {}".format( datum['auid'], bandgap, energycell))
AFLUX Server
Matchbook: materials keywords
Directive: return all entries satisfying query
JSON with query results is downloaded
F. Rose et al., Comput. Mater. Sci. 137, 362 (2017).

## Slide 51
AFLUX: AFLOW Search-API
G (p, T; V) = E + pV
Exercises:
Use AFLUX to retrieve the formation enthalpies for all of the entries in a ternary alloy system of your choice.
Use AFLUX to retrieve the space group numbers of all materials that contain Cu and Ti but not V (the logical NOT operator is denoted by the exclamation mark “!”).
Use AFLUX to retrieve the band gaps of all of the materials that have a calculated bulk modulus between 200GPa and 300GPa.
Use AFLUX to retrieve the materials in the ICSD catalog that contain the element Sn but not Pb, and that have a band gap between 1 and 3eV. How many such materials are available?
F. Rose et al., Comput. Mater. Sci. 137, 362 (2017).

## Slide 52
Outline
Getting started with AFLOW:
  Decorating crystal prototypes to set up new calculations
  Symmetry analysis
Thermodynamic and thermo-mechanical
  Convex hull phase diagrams
  AEL/AGL/APL: Elastic constants and thermal properties
AFLOW online data repositories
  AFLOW.org online web interface
  AFLOW REST-API
  AFLUX Search-API
AFLOW-ML + API
AFLOW code:
  Installing AFLOW
  Data analysis with AFLOW
  Running AFLOW calculations

## Slide 53
AFLOW Machine Learning
AFLOW data for > 26,674 materials on AFLOW.org used to train gradient boosting decision trees machine-learning model
Predictions based on structural morphology and elemental properties
O. Isayev et al., Nat. Commun. 8, 15679 (2017).
Voronoi tessellation used to determine atomic connectivity
Atoms which share a Voronoi cell face are connected to form a graph

## Slide 54
AFLOW Machine Learning
Connected atoms form structure fragments descriptors
O. Isayev et al., Nat. Commun. 8, 15679 (2017).
Atomic nodes in structure fragments are decorated with elemental properties to form Property-Labeled Materials Fragments (PLMF)
Properties used include number of valence electrons, ionization potential, electron affinity, electronegativity, covalent radii, etc.

## Slide 55
AFLOW Machine Learning
Model predicts electronic and thermo-mechanical properties
Model predicts electronic band gap for non-metals
O. Isayev et al., Nat. Commun. 8, 15679 (2017).

## Slide 56
AFLOW Machine Learning
ML model trained on 26674 unique GGA+U band structures from AFLOW.org to predict metal vs. insulator and electronic band gap
ML prediction vs. DFT+U calculation
Statistics for 5-fold cross-validation for electronic band gap:
RMSE: 0.51eV
MAE: 0.35eV
r2: 0.90
O. Isayev et al., Nat. Commun. 8, 15679 (2017).

## Slide 57
AFLOW Machine Learning
Partial dependence on elemental properties can be used to formulate design rules for new materials
Partial dependence:
metal vs. insulator
Partial dependence:
Band gap vs. ionization potential
O. Isayev et al., Nat. Commun. 8, 15679 (2017).

## Slide 58
AFLOW Machine Learning
Good agreement of predictions with both DFT and experiment
Partial dependence of properties on descriptors:
O. Isayev et al., Nat. Commun. 8, 15679 (2017).

## Slide 59
AFLOW.org: web portal
http://aflow.org
Machine-learning model
Curtarolo et al., Comput. Mater. Sci. 58, 218 (2012); Curtarolo et al., Comput. Mater. Sci. 58, 227 (2012)

## Slide 60
AFLOW-ML Online
Models are available online at aflow.org/aflow-ml
O. Isayev et al., Nat. Commun. 8, 15679 (2017), E. Gossett et al., Comput. Mater. Sci. 152, 134-145 (2018).

## Slide 61
AFLOW-ML API
Models are now programmatically accessible via AFLOW-ML API
E. Gossett et al., Comput. Mater. Sci. 152, 134-145 (2018).

## Slide 62
{
"id": "531c2817-ee51-4a23-be61-6e8ca6f31aec",
"model": "plmf",
"results_endpoint": "/prediction/result/531c2817-ee51-4a23-be61-6e8ca6f31aec"
}
AFLOW-ML API
Post POSCAR (for VASP version 5) to API using e.g. cURL:
E. Gossett et al., Comput. Mater. Sci. 152, 134-145 (2018).
> curl http://aflow.org/API/aflow-ml/v1.0/plmf/prediction
--data-urlencode file@POSCAR
Receive JSON file with task ID:
Mg1O1 [FCC,FCC,cF8] (STD_PRIM doi:10.1016/j.commatsci.2010.05.010)
1.224745
0.00000000000000 1.73622980869126 1.73622980869126
1.73622980869126 0.00000000000000 1.73622980869126
1.73622980869126 1.73622980869126 0.00000000000000
Mg O
1 1
Direct(2) [A1B1]
0.00000000000000 0.00000000000000 0.00000000000000 Mg
0.50000000000000 0.50000000000000 0.50000000000000 O

## Slide 63
AFLOW-ML API
Use task ID to query endpoint to retrieve results:
E. Gossett et al., Comput. Mater. Sci. 152, 134-145 (2018).
> curl http://aflow.org/API/aflow-ml/v1.0/prediction/result/531c2817-ee51-4a23-be61-6e8ca6f31aec
Receive JSON file with results:
{
"citation": "10.1038/ncomms15679",
"description": "The job has completed.",
"ml_ael_bulk_modulus_vrh": 144.522,
"ml_ael_shear_modulus_vrh": 104.453,
"ml_agl_debye": 777.163,
"ml_agl_heat_capacity_Cp_300K": 4.33,
"ml_agl_heat_capacity_Cp_300K_per_atom": 2.194,
"ml_agl_heat_capacity_Cv_300K": 4.178,
"ml_agl_heat_capacity_Cv_300K_per_atom": 2.139,
"ml_agl_thermal_conductivity_300K": 3.509,
"ml_agl_thermal_expansion_300K": 6.18e-05,
"ml_egap": 3.375,
"ml_egap_type": "Insulator",
"ml_energy_per_atom": -5.742,
"model": "plmf",
"status": "SUCCESS"
}

## Slide 64
AFLOW-ML API
Example python script to access AFLOW-ML API (part 1 of AFLOW-ML_example.py):
#!/usr/bin/env python
import json, sys, os
from urllib import urlopen
from urllib import urlencode
import urllib2
from time import sleep
SERVER="http://aflow.org"
API="/API/aflow-ml/v1.0"
MODEL="plmf"
poscar=open('POSCAR', 'r').read()
encoded_data = urlencode({'file': poscar,})
url = SERVER + API + "/" + MODEL + "/prediction"
request_task = urllib2.Request(url, encoded_data)
task = urllib2.urlopen(request_task).read()
task_json = json.loads(task)
results_endpoint = task_json["results_endpoint"]
results_url = SERVER + API + results_endpoint
AFLOW-ML API server
PLMF model
Read and encode POSCAR structure file
Post POSCAR to ML API server
Extract results endpoint from returned task object
E. Gossett et al., Comput. Mater. Sci. 152, 134-145 (2018).

## Slide 65
AFLOW-ML API
Example python script to access AFLOW-ML API (part 2 of AFLOW-ML_example.py):
incomplete = True
while incomplete:
request_results = urllib2.Request(results_url)
results = urllib2.urlopen(request_results).read()
results_json = json.loads(results)
if results_json["status"] == 'PENDING':
sleep(10)
continue
elif results_json["status"] == ’STARTED':
sleep(10)
continue
elif results_json["status"] == 'FAILURE':
print("Error: prediction failure")
incomplete = False
elif results_json["status"] == 'SUCCESS':
print("Successful prediction")
print(results_json)
incomplete = False
Query results endpoint until results are retrieved
If prediction is incomplete, wait and requery endpoint
Print error message for prediction failure
Print results for successful prediction
E. Gossett et al., Comput. Mater. Sci. 152, 134-145 (2018).

## Slide 66
AFLOW-ML API
AFLOW-ML API Python client can be downloaded from:
http://aflow.org/src/aflow-ml/
E. Gossett et al., Comput. Mater. Sci. 152, 134-145 (2018).

## Slide 67
AFLOW-ML API
AFLOW-ML API Python client can be installed using “setup.py” script included in client
python setup.py install
AFLOW-ML API Python client can be run using a script of this form:
from AFLOWml.client import AFLOWmlAPI
from pprint import pprint
with open('test.poscar', 'r') as input_file:
ml = AFLOWmlAPI()
data = ml.get_prediction(input_file.read(), 'plmf')
pprint(data)
E. Gossett et al., Comput. Mater. Sci. 152, 134-145 (2018).

## Slide 68
AFLOW-ML API
G (p, T; V) = E + pV
Exercises:
Convert the POSCAR files, generated previously using the AFLOW prototype modules, to the format used by version 5 of VASP by adding the additional line with the element symbols. Upload the POSCARs to the aflow.org/aflow-ml page, and generate predictions. Are these materials predicted to be metals or insulators?
Use the AFLOW-ML API to obtain predictions for both the plmf and mfd models for these structures, and retrieve the results in JSON format. For the structures generated using the prototype A_hR1_166_a, how does the value of c/a affect the elastic moduli and electronic band gap? What properties can you obtain using the mfd model?
E. Gossett et al., Comput. Mater. Sci. 152, 134-145 (2018).

## Slide 69
Outline
Getting started with AFLOW:
  Decorating crystal prototypes to set up new calculations
  Symmetry analysis
Thermodynamic and thermo-mechanical
  Convex hull phase diagrams
  AEL/AGL/APL: Elastic constants and thermal properties
AFLOW online data repositories
  AFLOW.org online web interface
  AFLOW REST-API
  AFLUX Search-API
AFLOW-ML + API
AFLOW code:
  Installing AFLOW
  Data analysis with AFLOW
  Running AFLOW calculations

## Slide 70
AFLOW: Installation
G (p, T; V) = E + pV
AFLOW can be installed using the xaflow script.
Install xaflow (perform once)
Curtarolo et al., Comput. Mater. Sci. 58, 218 (2012); Curtarolo et al., Comput. Mater. Sci. 58, 227 (2012)
1. Download xaflow:
wget materials.duke.edu/AFLOW/xaflow
2. Move/copy xaflow somewhere in your path:
mv xaflow /usr/local/bin/xaflow
3. Ensure the file can be executed:
chmod 555 /usr/local/bin/xaflow
4. Check that xaflow is in your path:
which xaflow
- A returned path means xaflow has been successfully installed.
5. Run xaflow:
xaflow
- xaflow downloads, unpacks, and makes AFLOW in
$(HOME)/src/AFLOW_local_YYMMDD_hhmm (Year, Month, Date, hour, minute).
- The compilation can be redirected to another path:
xaflow AWD=~/src/AFLOW_STANDARD
6. Install the newly compiled executable to your path:
xaflow install AWD=~/src/AFLOW_STANDARD
- By default, the executable is installed to /usr/local/bin.
- The installation can be redirected to another path:
xaflow install AWD=~/src/AFLOW_STANDARD ULB=~/bin
1. Download xaflow
2. Move/copy xaflow somewhere in your path
3. Ensure the file can be executed
4. Check that xaflow is in your path
wget materials.duke.edu/AFLOW/xaflow
mkdir ~/bin
export PATH=~/bin:$PATH
mv xaflow ~/bin/xaflow
chmod 555 ~/bin/xaflow
which xaflow

## Slide 71
AFLOW: Installation
G (p, T; V) = E + pV
Install AFLOW (perform with every new version)
Curtarolo et al., Comput. Mater. Sci. 58, 218 (2012); Curtarolo et al., Comput. Mater. Sci. 58, 227 (2012)
1. Download xaflow:
wget materials.duke.edu/AFLOW/xaflow
2. Move/copy xaflow somewhere in your path:
mv xaflow /usr/local/bin/xaflow
3. Ensure the file can be executed:
chmod 555 /usr/local/bin/xaflow
4. Check that xaflow is in your path:
which xaflow
- A returned path means xaflow has been successfully installed.
5. Run xaflow:
xaflow
- xaflow downloads, unpacks, and makes AFLOW in
$(HOME)/src/AFLOW_local_YYMMDD_hhmm (Year, Month, Date, hour, minute).
- The compilation can be redirected to another path:
xaflow AWD=~/src/AFLOW_STANDARD
6. Install the newly compiled executable to your path:
xaflow install AWD=~/src/AFLOW_STANDARD
- By default, the executable is installed to /usr/local/bin.
- The installation can be redirected to another path:
xaflow install AWD=~/src/AFLOW_STANDARD ULB=~/bin
1. Run xaflow
2. Install the newly compiled executable to your path
xaflow
xaflow install
- xaflow compiles AFLOW in ~/src/AFLOW by default
- To change the compilation directory, run
xaflow AWD=/home/src/AFLOW
- xaflow installs AFLOW to ~/bin by default
- To change the compilation directory, run
xaflow install ULB=/usr/local/bin
3. Run aflow
aflow

## Slide 72
AFLOW: Configuration
G (p, T; V) = E + pV
AFLOW can be configured with the .aflow.rc file
Curtarolo et al., Comput. Mater. Sci. 58, 218 (2012); Curtarolo et al., Comput. Mater. Sci. 58, 227 (2012)
1. Download xaflow:
wget materials.duke.edu/AFLOW/xaflow
2. Move/copy xaflow somewhere in your path:
mv xaflow /usr/local/bin/xaflow
3. Ensure the file can be executed:
chmod 555 /usr/local/bin/xaflow
4. Check that xaflow is in your path:
which xaflow
- A returned path means xaflow has been successfully installed.
5. Run xaflow:
xaflow
- xaflow downloads, unpacks, and makes AFLOW in
$(HOME)/src/AFLOW_local_YYMMDD_hhmm (Year, Month, Date, hour, minute).
- The compilation can be redirected to another path:
xaflow AWD=~/src/AFLOW_STANDARD
6. Install the newly compiled executable to your path:
xaflow install AWD=~/src/AFLOW_STANDARD
- By default, the executable is installed to /usr/local/bin.
- The installation can be redirected to another path:
xaflow install AWD=~/src/AFLOW_STANDARD ULB=~/bin
aflow --readme=aflowrc
VASP specific settings
  POTCAR paths (pseudo potentials files)
  Precision defaults (k-points scheme, minimization algorithm, energy cutoff, etc.)
  Run setting defaults (spin-polarized calculation, symmetry determination, etc.)
Machine settings
  MPI options
  Binary paths
  Database paths
AFLOW settings
  Output file names
  Graphic settings (Gnuplot, LaTeX)

## Slide 73
AFLOW: Crystallographic Prototypes
G (p, T; V) = E + pV
Decorate rock-salt prototype AB_cF8_225_a_b with MgO:
aflow --proto=AB_cF8_225_a_b:Mg:O --params=3.5
AB_cF8_225_a_b params=3.5 SG#=225 [ANRL doi: arXiv:1607.02532]
1.000000
0.00000000000000 1.75000000000000 1.75000000000000
1.75000000000000 0.00000000000000 1.75000000000000
1.75000000000000 1.75000000000000 0.00000000000000
1 1
Direct(2) [A1B1]
0.00000000000000 0.00000000000000 0.00000000000000 Mg
0.50000000000000 0.50000000000000 0.50000000000000 O
Use Heusler prototype T0001.A2BC to create aflow.in file for Cu2TiZn:
aflow --aflow_proto=T0001.A2BC:Cu:Ti:Zn
M. J. Mehl et al., Comput. Mater. Sci. 136, S1-S828 (2017); D. Hicks et al., submitted (2018)
Variety of possible ab-initio formats by adding options:
--vasp
VASP
--aims
FHI-AIMS
--qe
Quantum Espresso
--abinit
ABINIT

## Slide 74
AFLOW: High throughput aflow.in’s
G (p, T; V) = E + pV
Comma separated species
Pre-defined sets
aflow --aflow_proto=T0001.A2BC:Ag,Au,Cu,Fe:Mn,Ti:Zn
Curtarolo et al., Comput. Mater. Sci. 58, 218 (2012); Curtarolo et al., Comput. Mater. Sci. 58, 227 (2012)
Comma separated prototypes
aflow --aflow_proto=T0001.A2BC,TFCC001.ABC:Ag,Au,Cu,Fe:Mn,Ti:Zn
Full prototype listings
aflow --protos
AFLOW Standard
aflow --aflow_proto=T0001.A2BC:LIB3:LIB3:LIB3
http://aflow.org/CrystalDatabase
AFLOW Crystallographic Library
Have fun!

## Slide 75
AFLOW: Crystallographic Prototypes
G (p, T; V) = E + pV
Exercises:
Use the aflow --proto command with the appropriate options as described on the online prototype page to generate a POSCAR for the same structure used in the previous exercise, decorated with elements of your choice.
Generate structures for the prototype A_hR1_166_a using an element and value of a of your choice, with c/a values of 0.5, 0.612, 1.0, 1.225, 1.5, 2.45, and 3.0. Save these structures with appropriate names, as they will be used as part of a later exercise.
M. J. Mehl et al., Comput. Mater. Sci. 136, S1-S828 (2017); D. Hicks et al., submitted (2018)

## Slide 76
AFLOW-SYM
G (p, T; V) = E + pV
D. Hicks et al., Acta Cryst. A74, 184-203 (2018)
Point, factor, site-symmetry, and space group operations are calculated via:
aflow --aflowSYM < POSCAR
Tolerance values and output format can be set using the options:
aflow --aflowSYM=0.0001 --print=json < POSCAR
Space-group symmetry information (number/symbol, Wyckoff positions, cell setting, etc.) consistent with ITC conventions:
aflow --sgdata=0.0001 --print=json < POSCAR
Extended crystallographic data (crystal, lattice, superlattice, symmetry descriptions) can be extracted using:
aflow --edata=0.0001 --print=json < POSCAR
Other standalone symmetry commands:
aflow --aflowSG < POSCAR
Space-group number/symbol
aflow --wyccar < POSCAR
Wyckoff positions (POSCAR format)
aflow --pearson < POSCAR
Pearson symbol
aflow --sprim < POSCAR
Standard primitive cell

## Slide 77
AFLOW-CHULL: Convex Hull Phase Diagram
G (p, T; V) = E + pV
Output format can be specified as usual
Directly query a structure’s stability criterion
Directly query a structure’s distance from the hull
Directly query the energy of the hull at a particular stoichiometry
C. Oses et al., submitted arXiv:1806.06901 (2018)
High throughput inputs
aflow --chull --alloy=MnPd --print=json,txt,pdf
aflow --chull --alloy=MnPd --d2h=aflow:9001c322296fc162
aflow --chull --alloy=MnPd --sc=aflow:4fc97e549ca17d4e
aflow --chull --alloy=MnPd --hull_energy=0.25
aflow --chull --alloy=MnPt,PdPt
aflow --chull --alloy=Mn,Pd:Pt
aflow --chull --alloy=LIB2:LIB2
aflow --readme=chull
README for more options/help

## Slide 78
AFLOW: aflow.in file
G (p, T; V) = E + pV
The aflow.in file:
[AFLOW] **************************************************************************************************************
[AFLOW]SYSTEM=Cu_pvTi_svZn.T0001.A2BC
[AFLOW] **************************************************************************************************************
[AFLOW] input file for aflow
[AFLOW_MODE=VASP]
[AFLOW] **************************************************************************************************************
[AFLOW_MODE_ZIP=xz]
[AFLOW_MODE_BINARY=vasp46s]
[AFLOW] **************************************************************************************************************
[AFLOW] **************************************************************************************************************
#[AFLOW_MODE_MPI]
[AFLOW_MODE_MPI_MODE]NCPUS=MAX
[AFLOW_MODE_MPI_MODE]COMMAND ="mpirun -np"
[AFLOW_MODE_MPI_MODE]AUTOTUNE
[AFLOW_MODE_MPI_MODE]BINARY="mpivasp46s"
[AFLOW] **************************************************************************************************************
[AFLOW_SYMMETRY]CALC
#[AFLOW_SYMMETRY]SGROUP_WRITE
#[AFLOW_SYMMETRY]SGROUP_RADIUS=7.77
[AFLOW] **************************************************************************************************************
#[AFLOW_NEIGHBOURS]CALC
[AFLOW_NEIGHBOURS]RADIUS=7.7
[AFLOW_NEIGHBOURS]DRADIUS=0.1
[AFLOW] **************************************************************************************************************
#[AFLOW_APL]CALC // README_AFLOW_APL.TXT
[AFLOW_APL]ENGINE=DM // README_AFLOW_APL.TXT
[AFLOW_APL]DMAG=0.015 // README_AFLOW_APL.TXT
[AFLOW_APL]MINATOMS=100 // README_AFLOW_APL.TXT
#[AFLOW_APL]SUPERCELL=3x3x3 // README_AFLOW_APL.TXT
[AFLOW_APL]DC=y // README_AFLOW_APL.TXT
[AFLOW_APL]DPM=y // README_AFLOW_APL.TXT
[AFLOW_APL]ZEROSTATE=y // README_AFLOW_APL.TXT
[AFLOW_APL]DOS=y // README_AFLOW_APL.TXT
[AFLOW_APL]TP=y // README_AFLOW_APL.TXT
[AFLOW_APL]TPT=0:2000:10 // README_AFLOW_APL.TXT
System name

## Slide 79
AFLOW: aflow.in file
G (p, T; V) = E + pV
The aflow.in file:
[AFLOW] *************************************************************************************************************
[VASP_RUN]RELAX_STATIC_BANDS=2 // GENERATE | STATIC | RELAX=N | RELAX_STATIC=N | STATIC_BANDS | RELAX_STATIC_BANDS=N | REPEAT_BANDS [,DS[,DD[,DSCF]]]
[VASP_FORCE_OPTION]NEGLECT_NOMIX
#[VASP_FORCE_OPTION]KPOINTS=keyword[,keyword] // EVEN | ODD | KSHIFT_GAMMA_EVEN | KSHIFT_GAMMA_ODD | KSCHEME_MONKHORST_PACK | KSCHEME_GAMMA | GAMMA | KEEPK | IBZKPT
[VASP_FORCE_OPTION]SYM=ON // ON | OFF (default ON)
[VASP_FORCE_OPTION]AUTO_PSEUDOPOTENTIALS=potpaw_PBE // pot_LDA | pot_GGA | potpaw_LDA | potpaw_GGA | potpaw_PBE | potpaw_LDA_KIN | potpaw_PBE_KIN
[VASP_FORCE_OPTION]NBANDS // Estimate Bands (better than VASP)
#[VASP_FORCE_OPTION]PSTRESS=0.0 // Pressure in kBar (1kB=0.1GPa)
#[VASP_FORCE_OPTION]EDIFFG=-0.001 // EDIFFG for relaxed forces
#[VASP_FORCE_OPTION]ENMAX_MULTIPLY=1.4 // Multiplication of the max(pseudopotential_cutoffs)
#[VASP_FORCE_OPTION]POTIM=0.5 // ionic time-step
[VASP_FORCE_OPTION]SPIN=ON // (ON | OFF (default ON)), REMOVE_RELAX_1 | _2
#[VASP_FORCE_OPTION]AUTO_MAGMOM=ON // ON | OFF (default OFF)
[VASP_FORCE_OPTION]RELAX_MODE=ENERGY // (ENERGY | FORCES | ENERGY_FORCES | FORCES_ENERGY) (default: DEFAULT_VASP_FORCE_OPTION_RELAX_MODE_SCHEME in .aflow.rc)
[VASP_FORCE_OPTION]PREC=ACCURATE // (LOW | MEDIUM | NORMAL | HIGH | ACCURATE), PRESERVED (default: DEFAULT_VASP_FORCE_OPTION_PREC_SCHEME in .aflow.rc)
[VASP_FORCE_OPTION]ALGO=FAST // (NORMAL | VERYFAST | FAST | ALL | DAMPED), PRESERVED (default: DEFAULT_VASP_FORCE_OPTION_ALGO_SCHEME in .aflow.rc)
#[VASP_FORCE_OPTION]METAGGA=NONE // (TPSS | RTPSS | M06L | MBJL | SCAN | MS0 | MS1 | MS2 | NONE) (default: DEFAULT_VASP_FORCE_OPTION_METAGGA_SCHEME in .aflow.rc)
#[VASP_FORCE_OPTION]IVDW=0 // (number_for_VASP_see_manual_for_IVDW | 0) (default: DEFAULT_VASP_FORCE_OPTION_IVDW_SCHEME in .aflow.rc)
[VASP_FORCE_OPTION]RELAX_ALL
#[VASP_FORCE_OPTION]NOTUNE
[VASP_FORCE_OPTION]TYPE=DEFAULT // (METAL | INSULATOR | SEMICONDUCTOR | DEFAULT) (default DEFAULT)
[VASP_FORCE_OPTION]CONVERT_UNIT_CELL=SPRIM,MINK // (SPRIM, SCONV, NIGGLI, MINK, INCELL, COMPACT, WS, CART, FRAC, PRES)
#[VASP_FORCE_OPTION]VOLUME+=10.0
[VASP_FORCE_OPTION]VOLUME*=1.05
[AFLOW] *************************************************************************************************************
Calculation type
Exchange-correlation functional
Relaxation mode
Basis cut-off

## Slide 80
AFLOW: aflow.in file
G (p, T; V) = E + pV
The aflow.in file:
[AFLOW] *************************************************************************************************************
[VASP_INCAR_MODE_EXPLICIT]START
SYSTEM=Cu_pvTi_svZn.T0001.A2BC
#PSTRESS=000 # Pressure in kBar (1kB=0.1GPa) # for hand modification
#EDIFFG=-0.001 # For relaxed forces # for hand modification
#POTIM=-0.001 # default # for hand modification
#NBANDS=XX # for hand modification
#IALGO=48 # for hand modification
[VASP_INCAR_MODE_EXPLICIT]STOP
[AFLOW] *************************************************************************************************************
[VASP_KPOINTS_MODE_IMPLICIT]
[VASP_KPOINTS_FILE]KSCHEME=M
[VASP_KPOINTS_FILE]KPPRA=6000
[VASP_KPOINTS_FILE]STATIC_KSCHEME=M
[VASP_KPOINTS_FILE]STATIC_KPPRA=10000
[VASP_KPOINTS_FILE]BANDS_LATTICE=AUTO
[VASP_KPOINTS_FILE]BANDS_GRID=20
[AFLOW] *************************************************************************************************************
Explicit INCAR additions
k-point grid settings

## Slide 81
AFLOW: aflow.in file
G (p, T; V) = E + pV
The aflow.in file:
[AFLOW] *************************************************************************************************************
[VASP_POSCAR_MODE_EXPLICIT]START
Cu_pvTi_svZn/T0001.A2BC - (T0001.A2BC) - AlCu2Mn [A2BC] (T0001.A2BC) & Fm(-3)m & #225 & cF16 & Navy HTQC Project (use of T0001.proto)
-56.218000
0.00000000000000 1.00000000000000 1.00000000000000
1.00000000000000 0.00000000000000 1.00000000000000
1.00000000000000 1.00000000000000 0.00000000000000
2 1 1
Direct(4) [A2B1C1]
0.75000000000000 0.75000000000000 0.75000000000000 Cu_pv
0.25000000000000 0.25000000000000 0.25000000000000 Cu_pv
0.00000000000000 0.00000000000000 0.00000000000000 Ti_sv
0.50000000000000 0.50000000000000 0.50000000000000 Zn
[VASP_POSCAR_MODE_EXPLICIT]STOP
[AFLOW] *************************************************************************************************************
[VASP_POTCAR_MODE_IMPLICIT]
[VASP_POTCAR_FILE]Cu
[VASP_POTCAR_FILE]Ti
[VASP_POTCAR_FILE]Zn
[AFLOW] potpaw_PBE: Cu_pv Ti_sv Zn
[AFLOW] COMPOSITION_PP=|Cu_pv2|Ti_sv1|Zn1|
[AFLOW] COMPOSITION=|Cu2|Ti1|Zn1|
[AFLOW] VOLUME(A^3)=|12.0159|17.1035|15.0827|
[AFLOW] MASS(amu)=|63.546|47.9|65.38|
[AFLOW] *************************************************************************************************************
POSCAR: VASP geometry input file
POTCAR: VASP pseudopotential

## Slide 82
AFLOW creates a “LOCK” file in directories when it starts to run VASP, preventing future AFLOW runs in that directory. To run, e.g., an APL (phonon) calculation in the same directory, change the name used for the LOCK file as follows:
Running AFLOW
G (p, T; V) = E + pV
VASP calculations can be run through AFLOW using commands of this form:
The AFLOW monitor option can be used to monitor jobs to prevent them consuming excessive resources and crashing the computer:
A typical job submission script should contain something like the following:
aflow --run --force --D <run directory path>
aflow --monitor
touch log.$PBS_JOBID
aflow --monitor >> log.$PBS_JOBID &
aflow --run --force --D ./ >> log.$PBS_JOBID
aflow --use_LOCK=apl.LOCK --multi --D <run directory path>

## Slide 83
aflow --multi --D <directory path>
AEL: Elastic constants
G (p, T; V) = E + pV
AFLOW-AEL is run by including the following line in the aflow.in:
[AFLOW_AEL]CALC
The number and size of the normal and shear strains can be set using the following lines:
[AFLOW_AEL]NNORMALSTRAINS=<number>
[AFLOW_AEL]NSHEARSTRAINS=<number>
[AFLOW_AEL]NORMALSTRAINSTEP=<number>
[AFLOW_AEL]SHEARSTRAINSTEP=<number>
Symmetry can be used to reduce the number of independent directions by including the following lines:
[AFLOW_AEL]STRAINSYMMETRY=ON
DFT calculations can be run for the strained structures in all of the subdirectories using the following command:
C. Toher et al., Phys. Rev. Mater. 1, 015401 (2017)

## Slide 84
AEL: Elastic constants
G (p, T; V) = E + pV
Exercises:
Add the appropriate line to run an AEL calculation to the aflow.in file created using the Heusler prototype in the previous exercise.
Use the command aflow --run --generate_aflowin_only to create the subdirectories for this AEL calculation. (Note: this will not perform any DFT calculations, which would require VASP to be installed on your computer and can be computationally expensive. To run DFT calculations, leave out the option --generate_aflowin_only. Use the command aflow --multi --D ./ to run all subdirectories). How many subdirectories are created?
Copy the aflow.in file to a new directory, and add the option to switch on the use of symmetry to determine number of independent directions. Re-run the command to generate the subdirectories. How many subdirectories are created now?
C. Toher et al., Phys. Rev. Mater. 1, 015401 (2017)

## Slide 85
AGL: Debye-Grüneisen model
G (p, T; V) = E + pV
AFLOW-AGL is run by including the following line in the aflow.in:
[AFLOW_AGL]CALC
The number and size of the isotropic strains applied to the structures can be set using the following lines:
[AFLOW_AGL]NSTRUCTURES=<number>
[AFLOW_AGL]STRAINSTEP=<number>
The value of the Poisson ratio used to calculate the Debye temperature can be set using the following line:
[AFLOW_AGL]POISSON=<number>
DFT calculations can be run for the strained structures using the following command:
C. Toher et al., Phys. Rev. B 90, 174107 (2014); C. Toher et al., Phys. Rev. Mater. 1, 015401 (2017)
AEL can be called to calculate the Poisson ratio using the following line:
[AFLOW_AGL]AELPOISSONRATIO=ON
aflow --multi --D <directory path>

## Slide 86
AGL: Debye-Grüneisen model
G (p, T; V) = E + pV
Exercises:
Add the appropriate line to run an AGL calculation to the aflow.in file created using the Heusler prototype in the previous exercise.
Use the command aflow --run --generate_aflowin_only to create the subdirectories for this calculation. (Note: this will not perform any DFT calculations, which would require VASP to be installed on your computer and can be computationally expensive. To run DFT calculations, leave out the option --generate_aflowin_only. Use the command aflow --multi --D ./ to run all subdirectories). How many subdirectories are created?
Copy the aflow.in file to a new directory, and add the option to use AEL to calculate the Poisson ratio. Re-run the command to generate the subdirectories. What structures are created?
C. Toher et al., Phys. Rev. B 90, 174107 (2014); C. Toher et al., Phys. Rev. Mater. 1, 015401 (2017)

## Slide 87
APL: Phonon calculations
G (p, T; V) = E + pV
AFLOW-APL is run by uncommenting the following line in the aflow.in:
[AFLOW_APL]CALC
Additional parameters:
[AFLOW_APL]ENGINE=DM
[AFLOW_APL]DMAG=0.015
[AFLOW_APL]MINATOMS=100
#[AFLOW_APL]SUPERCELL=3x3x3
[AFLOW_APL]DC=y
[AFLOW_APL]DCUSERPATH=G-X|X-U|K-G|G-L
[AFLOW_APL]DPM=y
[AFLOW_APL]ZEROSTATE=y
[AFLOW_APL]POLAR=y
[AFLOW_APL]DOS=y
[AFLOW_APL]TP=y
[AFLOW_APL]TPT=0:2000:10
[AFLOW_APL]KPPRA=2000
Followed by the usual run command
aflow --run --LOCK=apl.LOCK
Curtarolo et al., Comput. Mater. Sci. 58, 218 (2012); Curtarolo et al., Comput. Mater. Sci. 58, 227 (2012)

## Slide 88
APL: Phonon calculations
G (p, T; V) = E + pV
DFT calculations can be run for the strained structures using the following command:
Alternatively, a fresh aflow.in can be created with the line already uncommented
aflow --aflow_proto=T0001.A2BC:Cu:Ti:Zn --module=apl
aflow --multi --D <directory path>

## Slide 89
APL: Phonon calculations
G (p, T; V) = E + pV
Exercises:
Add/uncomment the appropriate line to run an APL calculation to the aflow.in file created using the Heusler prototype in the previous exercise.
Use the command aflow --run --generate_aflowin_only to create the subdirectories for this calculation. (Note: this will not perform any DFT calculations, which would require VASP to be installed on your computer and can be computationally expensive. To run DFT calculations, leave out the option --generate_aflowin_only. Use the command aflow --multi --D ./ to run all subdirectories). How many subdirectories are created? How many atoms do the supercells contain?

## Slide 90
Conclusions
G (p, T; V) = E + pV
Automatic materials design frameworks can generate large quantities of materials data and combine multiple DFT calculations to predict thermodynamic stability and thermo-mechanical properties
AFLOW data is accessible via aflow.org web portal, AFLOW REST-API, and AFLUX Search-API
Calculated AFLOW data for electronic and thermo-mechanical properties is being used to train machine-learning models to predict these quantities, which are accessible by AFLOW-ML API

## Slide 91
Acknowledgements
Prof. Stefano Curtarolo (Duke): Director, Center for Materials Genomics
Dr. Frisco Rose (Duke): AFLUX Search-API
Eric Gossett (Duke): convex hull online application, online ML application, AFLOW-ML API
Prof. M. Mehl, (US Naval Academy): library of crystal prototypes
Dr. O. Isayev, Prof. A. Tropsha (UNC Chapel Hill): PLMF machine learning models
Dr. F. Legrain, Dr. J. Carrete, Dr. N. Mingo (CEA Grenoble): MFD machine learning model